# Text boxes

# Product Data Sheet ZP24-80-3
Serial # 1132.2-5

Thank you for your purchase of an Xradia zone plate optic. In this document you find the parameters and fabrication tolerances of the zone plate.

## Zone Plate Parameters:

| Outer Diameter | m | 80 |
| --- | --- | --- |
| Inner Diameter (no zones) | m | N/A |
| Outermost Zone Width | nm | 24 |
| Zone Material |  | Electroplated Gold |
| Zone Height | nm | 300 +/- 8% |
| Number Of Zones2 |  | 833 |
| Suggested Energy Range3 | keV |  |
| Theoretical Max. Diffraction Efficiency1 | % |  |
| Support Membrane Material |  | Si3N4 |
| Support Membrane Thickness | m | 0.1 |
| Support Membrane Size | mm | 0.2 x 0.2 |
| Support Silicon Frame Size | mm | 2 x 2 |
| Central Stop Diameter4 | m | NA |
| Central Stop Height / Material | m | NA |

1 Xradia delivers zone plates with a focusing efficiency exceeding 50% of the theoretically calculated value.

2 Number of fabricated rings calculated for a full zone plate (no missing inner zones).

3 Energy range for which the theoretical efficiency is greater 10%.

4 The placement accuracy of the stop is 10m (typical 5 m).

## Zone Plate Focal Length

The focal length of the zone plate is given by:

# Product Data Sheet ZP24-80-3
Serial # 1132.2-5

## Use In Vacuum

Zone plates can be used in vacuum. Several precautions need to be taken:

- No pressure differential can be applied between both sides of the zone plate wafer.

- Change the ambient pressure slowly. Avoid shocks generated by opening large conductance pneumatic valves.

- Zone plates can be damaged by ultra-sonic particles generated during venting of the vacuum system. Vent slowly and with a clean gas (use filter if possible). Avoid venting through a port which is in direct line-of-sight of the zone plate. Install a shield if necessary.

- Make sure that the zone plate heat load is small and removed through proper thermal connections. If in doubt, consult Xradia for advice.

## SEM Micrograph

Outermost zones of the zone plate